# Version: 01/09/02

Heatset Ink Series

“CALORAMA”

# DESCRIPTION

________________________________________________________________________________

Heat-Set ink series suitable for printing on LWC and SC papers. Designed for last generation High Speed Presses (Heidelberg Sunday M4000, Lithoman IV 48/64 pp, KBA Compacta 618). Main features are the wide application range and the reduced misting at high speed. Fast heat reaction.

________________________________________________________________________________

# SHADES

________________________________________________________________________________

| - Yellow 2520 HS J950 C96010110 | - Red 2521 Calorama 2000 C96030200 |
| --- | --- |
| - Blue 2522 Calorama 2000 C96020200 | - Black HS 3000 Calorama 950 C96040230 |

________________________________________________________________________________

# PROPERTIES

________________________________________________________________________________

| - Excellent behaviour on press | - Outstanding ink/water balance |
| --- | --- |
| - Reduced Dot Gain | - Outstanding ink trapping |
| - Smooth ink layer | - Good Drying |
| - Good Rub resistance | - Good Gloss level |

________________________________________________________________________________

# TECHNICAL DATA

____________________________________________________________________

- Tack (300 m/min)			: 175-190

- ViscositY (Laray, 25°C)		: 125-135 Poises

- Yield Value (Laray, 25°C)		: 2250-2750 dynes/cm2

____________________________________________________________________